Copyright 2009 by The American Institute of Architects (AIA)

Exclusively published and distributed by Architectural Computer Services, Inc. (ARCOM) for the AIA

SECTION 034500 - PRECAST ARCHITECTURAL CONCRETE

This Section uses the term "Architect."  Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

- GENERAL

      - RELATED DOCUMENTS

        - Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 01 Specification Sections, apply to this Section.

      - SUMMARY

        - This Section includes the following:

Adjust list below to suit Project.

          - Precast Concrete Stairs and Landings

          - [Insert Additional Precast Unit Types]

        - Related Sections include the following:

List below only products and construction that the reader might expect to find in this Section but are specified elsewhere.

          - Division 03 Section "Cast-In-Place Concrete" for installing connection anchors in concrete.

          - Division 05 Section "Structural Steel Framing" for furnishing and installing connections attached to structural-steel framing.

          - Division 05 Section "Metal Fabrications" for kickers and other miscellaneous steel shapes.

      - DEFINITION

Retain this Article if a design reference sample has been preapproved by Architect.

        - Design Reference Sample:  Sample of approved architectural precast concrete color, finish and texture, provided by Northwest Precast and preapproved by Architect.

      - PERFORMANCE REQUIREMENTS

        - Structural Performance:  Provide architectural precast concrete units and connections capable of withstanding the following design loads within limits and under conditions indicated:

          - Loads:  As indicated on structural drawings.

Retain subparagraph above if design loads are shown on Drawings or delete subparagraph above and retain first five subparagraphs below if including design loads here; revise requirements to suit Project, and add other performance and design criteria if applicable.

Revise subparagraph below to suit local conditions.  Temperature data are available from National Climatic Data Center, www.ncdc.noaa.gov.

Delete subparagraph below if window washing system is not required.  Indicate design criteria here or on Drawings for window washing system, including material and equipment.

      - ACTION SUBMITTALS

        - Product Data:  For each type of product indicated.

        - Design Mixtures:  For each precast concrete mixture.  Include compressive strength and water-absorption tests.

        - Shop Drawings:  Detail fabrication and installation of architectural precast concrete units.  Indicate locations, plans, elevations, dimensions, shapes, and cross sections of each unit.  Indicate joints, reveals, and extent and location of each surface finish.  Indicate details at building corners.

Delete subparagraphs below not applicable to Project.

          - Indicate separate face and backup mixture locations and thicknesses.

          - Indicate welded connections by AWS standard symbols.  Detail loose and cast-in hardware and connections.

          - Indicate locations, tolerances, and details of anchorage devices to be embedded in or attached to structure or other construction.

          - Indicate locations, extent, and treatment of dry joints if two-stage casting is proposed.

          - Include plans and elevations showing unit location and sequence of erection for special conditions.

          - Indicate location of each architectural precast concrete unit by same identification mark placed on panel.

          - Indicate relationship of architectural precast concrete units to adjacent materials.

          - Indicate locations and details of brick units, including corner units and special shapes, and joint treatment.

          - Indicate locations and details of stone facings, anchors, and joint widths.

          - Design Modifications:  If design modifications are proposed to meet performance requirements and field conditions, submit design calculations and Shop Drawings.  Do not adversely affect the appearance, durability, or strength of units when modifying details or materials and maintain the general design concept.

Retain subparagraph below if retaining "Performance Requirements" Article.  Delete or modify if Architect assumes or is required by law to assume design responsibility.

          - Comprehensive engineering analysis signed and sealed certified by the qualified professional engineer licensed responsible for its preparation. The design professional shall be licensed within the state that the project is located.  The calculations shall indicated review of governing panel types, connections, and types of reinforcement, including special reinforcement.  Indicate location, type, magnitude, and direction of loads imposed on the building structural frame from architectural precast concrete.

          - When required submit additional shop drawings and calculations for jurisdictional review.

Retain paragraph and subparagraphs below if finishes, colors, and textures are preselected, specified, or scheduled.  Coordinate with sample panels and range samples in "Quality Assurance" Article.

        - Samples:  For each type of finish indicated on exposed surfaces of architectural precast concrete units, in sets of 3, illustrating full range of finish, color, and texture variations expected; approximately 12 by 12 by 2-inches.

          - When other faces of precast concrete unit are exposed, include Samples illustrating workmanship, color, and texture of backup concrete as well as facing concrete.

      - INFORMATIONAL SUBMITTALS

Coordinate first paragraph below with qualification requirements in Division 01 Section "Quality Requirements" and as supplemented in "Quality Assurance" Article.

        - Qualification Data:  For Installer, fabricator and testing agency.

Retain paragraph below if procedures for welder certification are retained in "Quality Assurance" Article.

        - Welding certificates.

        - Material Certificates:  For the following items, signed by manufacturers:

Edit list below to suit Project.

          - Cementitious materials.

          - Reinforcing materials.

          - Admixtures.

          - Bearing pads.

          - Structural-steel shapes and hollow structural sections.

          - Stone anchors.

        - Material Test Reports:  For aggregates.

Retain paragraph below if submittal is required.

        - Source quality-control test reports.

Retain paragraph below if Contractor is responsible for field quality-control testing.  Retain option if Contractor is responsible for special inspections.

        - Field quality-control test and special inspection reports.

      - QUALITY ASSURANCE

        - Fabricator qualifications:  The bidding firm shall participate in the Architectural Precast Association (APA) “Plant Certification Program of Architectural Precast Concrete Products” and is designated as a APA-Certified Plant. The bidding firm responsibility includes preparing of shop drawings and comprehensive engineering analysis by a qualified professional engineer.  They shall demonstrate a minimum of 5 years experience in producing units similar to those required for this project.

          - Acceptable Manufacturers:

            - Northwest Precast

- Corporate Office:					Manufacturing:

- 2323 West Overland Road			212 10th Street SE

- Boise, ID 83705					      Puyallup, WA 98372

- (800) 771-4862					     (253) 770-9119

- (208) 472-0042					     (253) 770-3826 Fax

- (208) 331-8301 Fax

Retain one of first two paragraphs below if qualifying erectors.  Retain first if PCI-certified erector is required.  See PCI's Web site, www.pci.org, for current listing of erectors.

        - Installer Qualifications:  Installer shall demonstrate a record of at least five years of successful installation of precast units similar to those required for this project.

Retain first paragraph below if PCI-certified erector is not required or is not available in Project location.  Basis of audit is PCI MNL 127, "PCI Erector's Manual - Standards and Guidelines for the Erection of Precast Concrete Products."

        - Fabricator Qualifications: A firm that assumes responsibility for engineering architectural precast concrete units to comply with performance requirements.  This responsibility includes preparation of Shop Drawings and comprehensive engineering analysis by a qualified professional engineer.

Usually retain subparagraph below.  PCI plant certification was established in 1967 and is a different program than APA's plant certification established in 1993.  Consult APA or PCI for further information.

Retain first paragraph below if Contractor selects testing agency for testing in addition to that required under PCI's certification program.  Testing agency is normally engaged by Owner.

        - Testing Agency Qualifications:  An independent testing agency acceptable to authorities having jurisdiction, qualified according to ASTM C 1077 and ASTM E 329 for testing indicated.

        - Quality-Control Standard:  For manufacturing procedures and testing requirements, quality-control recommendations, and dimensional tolerances for types of units required, comply with PCI MNL 117, "Manual for Quality Control for Plants and Production of Architectural Precast Concrete Products."

Delete paragraph below if no welding.  Retain "Welding certificates" Paragraph in "Informational Submittals" Article if retaining below.  AWS states that welding qualifications remain in effect indefinitely unless welding personnel have not welded for more than six months or there is a specific reason to question their ability.

        - Welding:  Qualify procedures and personnel according to AWS D1.1/D.1.1M, "Structural Welding Code - Steel"; and AWS D1.4, "Structural Welding Code - Reinforcing Steel."

PCI recommends review of preproduction sample panels.  Revise number and size of sample panels in paragraph below to suit Project.

        - Sample Panels:  After sample approval and before fabricating architectural precast concrete units, produce a minimum of 2 sample panels approximately 16 sq. ft. in area for review by Architect.  Incorporate full-scale details of architectural features, finishes, textures, and transitions in sample panels.

          - Locate panels where indicated or, if not indicated, as directed by Architect.

          - Damage part of an exposed-face surface for each finish, color, and texture, and demonstrate adequacy of repair techniques proposed for repair of surface blemishes.

          - After acceptance of repair technique, maintain one sample panel at manufacturer's plant and one at Project site in an undisturbed condition as a standard for judging the completed Work.

          - Demolish and remove sample panels when directed.

Delete paragraph and subparagraphs below if sample panels and range samples above will suffice and added expense of mockups is not required.  If retaining, indicate location, size, and other details of mockups on Drawings or by inserts.  Revise wording if only one mockup is required.

        - Mockups:  After sample panel approval but before production of architectural precast concrete units, construct full-sized mockups to verify selections made under sample submittals and to demonstrate aesthetic effects and set quality standards for materials and execution.

Revise or delete three subparagraphs below to suit Project.

          - Build mockup as indicated on Drawings of architectural precast concrete complete with anchors, connections, flashings, and joint fillers.

Retain first subparagraph below if mockups are erected as part of building rather than separately and the intention is to make an exception to the default requirement in Division 01 Section "Quality Requirements" for demolishing and removing mockups when directed, unless otherwise indicated.

          - Approved mockups may become part of the completed Work if undamaged at time of Substantial Completion.

          - Approval of mockups does not constitute approval of deviations from the Contract Documents unless such deviations are specifically approved by Architect in writing.

If retaining paragraph and subparagraphs below, determine where preconstruction testing will be specified and include requirements in that Section.  Requirements in paragraph below are limited to building a preconstruction testing mockup at a testing agency's facility.

        - Preconstruction Testing Mockup:  Provide a full-size mockup of architectural precast concrete indicated on Drawings for preconstruction testing.  Refer to Division [01] [08] <Insert Division number> Section "<Insert Section title>" for preconstruction testing requirements.

Revise or delete subparagraphs below to suit Project.  Coordinate with other Sections that include construction to be included in a preconstruction testing mockup to clearly indicate extent of work required in this Section.

          - Build preconstruction testing mockup size and design determined as indicated on Drawings including aluminum framing, glass, sealants. Architectural precast concrete mock-up to be complete with anchors, connections, flashings, and joint fillers.  Mockup color and finish to  match the design reference sample.

          - Build preconstruction testing mockup at testing agency facility.

Delete paragraph below if Work of this Section is not extensive or complex enough to justify a preinstallation conference.  If retaining, coordinate with Division 01.

        - Preinstallation Conference:  Conduct conference at Project site to comply with requirements in Division 01 Section "Project Management And Coordination."

      - DELIVERY, STORAGE, AND HANDLING

        - Deliver architectural precast concrete units in such quantities and at such times to limit unloading units temporarily on the ground.

        - Support units during shipment on nonstaining shock-absorbing material.

        - Store units with adequate dunnage and bracing and protect units to prevent contact with soil, to prevent staining, and to prevent cracking, distortion, warping or other physical damage.

        - Place stored units so identification marks are clearly visible, and units can be inspected.

        - Handle and transport units in a position consistent with their shape and design in order to avoid excessive stresses which would cause cracking or damage.

        - Lift and support units only at designated points shown on Shop Drawings.

      - SEQUENCING

        - Furnish loose connection hardware and anchorage items to be embedded in or attached to other construction without delaying the Work.  Provide locations, setting diagrams, templates, instructions, and directions, as required, for installation.

- PRODUCTS

      - MOLD MATERIALS

        - Molds:  Rigid, dimensionally stable, non-absorptive material, warp and buckle free, that will provide continuous and true precast concrete surfaces within fabrication tolerances indicated; nonreactive with concrete and suitable for producing required finishes.

          - Mold-Release Agent:  Commercially produced liquid-release agent that will not bond with, stain or adversely affect precast concrete surfaces and will not impair subsequent surface or joint treatments of precast concrete.

Delete paragraph below if not using form liners.  Form liners may be used to achieve a special off-the-form finish or to act as a template for thin or half-brick facings.  Revise to add description of selected form liner if required.

        - Form Liners:  Units of face design, texture, arrangement, and configuration to match design reference sample.  Furnish with manufacturer's recommended liquid-release agent that will not bond with, stain, or adversely affect precast concrete surfaces and will not impair subsequent surface or joint treatments of precast concrete.

      - REINFORCING MATERIALS

Select one or more paragraphs in this Article to suit steel reinforcement requirements.  Distinguish locations of each type of reinforcement here or on Drawings.  If retaining Part 1 "Performance Requirements" Article, consider reviewing selections with fabricators.

        - Reinforcing Bars:  ASTM A 615/A 615M, Grade 60, deformed.

Retain paragraph below for reinforcement that is welded or if added ductility is sought.

        - Low-Alloy-Steel Reinforcing Bars:  ASTM A 615/A 615M, Grade 60, deformed.

        - Steel Bar Mats:  ASTM A 184/A 184M, fabricated from ASTM A 615/A 615M, Grade 60,, deformed bars, assembled with clips.

        - Plain-Steel Welded Wire Reinforcement:  ASTM A 185, fabricated from as-drawn steel wire into flat sheets.

        - Deformed-Steel Welded Wire Reinforcement:  ASTM A 497/A 497M, flat sheet.

        - Supports:  Suspend reinforcement from back of mold or use bolsters, chairs, spacers, and other devices for spacing, supporting, and fastening reinforcing bars and welded wire reinforcement in place according to PCI MNL 117.

      - CONCRETE MATERIALS

Delete materials in this Article that are not required; revise to suit Project.

        - Portland Cement:  ASTM C 150, Type I or Type III, gray or white based on architects selection. Use only one brand type and color from same mill.

Mixing with white cement will improve color uniformity of gray cement.  White cement has greater color consistency than gray cement and should be used for pastel colors.  For darker colors, variations of gray cement have less effect on final color hue.

        - Supplementary Cementitious Materials:

Select mineral or cementitious admixtures from four subparagraphs below.  Because fly ash, silica fume, and ground slag affect color uniformity, they are not recommended by PCI where appearance is important.

          - Fly Ash:  ASTM C 618, Class C or F, with maximum loss on ignition of 3 percent.

          - Metakaolin Admixture:  ASTM C 618, Class N.

          - Silica Fume Admixture:  ASTM C 1240, with optional chemical and physical requirement.

          - Ground Granulated Blast-Furnace Slag:  ASTM C 989, Grade 100 or 120.

ASTM C 33 limits deleterious substances in coarse aggregate depending on climate severity and in-service location of concrete.  Class 5S is the most restrictive designation for architectural concrete exposed to severe weathering.  PCI MNL 117 also establishes strict limits on deleterious substances for fine and coarse aggregates.

        - Normal-Weight Aggregates:  Except as modified by PCI MNL 117, ASTM C 33, with coarse aggregates complying with Class 5S.  Stockpile fine and coarse aggregates for each type of exposed finish from a single source (pit or quarry) for Project to match design reference sample mix design.

Revise two subparagraphs below to add descriptions of selected coarse- and fine-face aggregate colors and sources if required.

          - Face-Mixture-Coarse Aggregates:  Selected, hard, and durable; free of material that reacts with cement or causes staining; to match design mix of the design reference.

Retain one option from first subparagraph below or insert gradation and maximum aggregate size if known.  Fine and coarse aggregates are not always from same source.

            - Gradation:  To match design reference sample.

          - Face-Mixture-Fine Aggregates:  Selected, natural or manufactured sand of same material as coarse aggregate, to match design reference sample, unless otherwise approved by the Architect.

Delete first paragraph below if coloring admixture is not required.  Add color selection if known.

        - Coloring Admixture:  ASTM C 979, synthetic or natural mineral-oxide pigments or colored water-reducing admixtures, temperature stable, and nonfading.

        - Water:  Potable; free from deleterious material that may affect color stability, setting, or strength of concrete and complying with chemical limits of PCI MNL 117.

        - Air-Entraining Admixture:  ASTM C 260, certified by manufacturer to be compatible with other required admixtures.

        - Chemical Admixtures:  Certified by manufacturer to be compatible with other admixtures and to not contain calcium chloride, or more than 0.15 percent chloride ions or other salts by weight of admixture.

Select one or more chemical admixtures from seven subparagraphs below if chemical admixtures are permitted; limit chemical admixture types if required.  Water-reducing admixtures, Types A, D, and E, or a high-range water reducer, Type F, predominate.

          - Water-Reducing Admixtures:  ASTM C 494/C 494M, Type A.

          - Retarding Admixture:  ASTM C 494/C 494M, Type B.

          - Water-Reducing and Retarding Admixture:  ASTM C 494/C 494M, Type D.

          - Water-Reducing and Accelerating Admixture:  ASTM C 494/C 494M, Type E.

          - High-Range, Water-Reducing Admixture:  ASTM C 494/C 494M, Type F.

          - High-Range, Water-Reducing and Retarding Admixture:  ASTM C 494/C 494M, Type G.

          - Plasticizing and Retarding Admixture:  ASTM C 1017/C 1017 M.

      - STEEL CONNECTION MATERIALS

        - As indicated on drawings.

Edit this Article to suit Project.  Add other materials as required.

        - Carbon-Steel Shapes and Plates:  ASTM A 36/A 36M.

        - Carbon-Steel-Headed Studs:  ASTM A 108, AISI 1018 through AISI 1020, cold finished, AWS D1.1/D1.1M, Type A or B, with arc shields and with minimum mechanical properties of PCI MNL 117, Table 3.2.3.

        - Carbon-Steel Plate:  ASTM A 283/A 283M.

        - Malleable Iron Castings:  ASTM A 47/A 47M.

        - Carbon-Steel Castings:  ASTM A 27/A 27M, Grade 60-30.

        - High-Strength, Low-Alloy Structural Steel:  ASTM A 572/A 572M.

        - Carbon-Steel Structural Tubing:  ASTM A 500, Grade B.

        - Wrought Carbon-Steel Bars:  ASTM A 675/A 675M, Grade 65.

        - Deformed-Steel Wire or Bar Anchors:  ASTM A 496 or ASTM A 706/A 706M.

ASTM A 307 defines the term "studs" to include stud stock and threaded rods.

        - Carbon-Steel Bolts and Studs:  ASTM A 307, Grade; carbon-steel, hex-head bolts and studs; carbon-steel nuts, ASTM A 563; and flat, unhardened steel washers, ASTM F 844.

High-strength bolts are used for friction-type connections between steel members and are not recommended by PCI between steel and concrete because concrete creep and crushing of concrete during bolt tightening reduce effectiveness.

        - High-Strength Bolts and Nuts:  ASTM A 325, Type 1, heavy hex steel structural bolts; heavy hex carbon-steel nuts, ASTM A 563; and hardened carbon-steel washers, ASTM F 436.

Retain first paragraph below if paint finish is required.  Revise locations of priming if required.  MPI 79 in first option provides some corrosion protection, while SSPC-Paint 25, without topcoating, provides minimal corrosion protection.

        - Shop-Primed Finish:  Prepare surfaces of nongalvanized steel items, except those surfaces to be embedded in concrete, according to requirements in SSPC-SP 3 and shop-apply [lead- and chromate-free, rust-inhibitive primer, complying with performance requirements in MPI 79, SSPC-Paint 25 according to SSPC-PA 1.

        - Welding Electrodes:  Comply with AWS standards.

      - HOT-DIP GALVINIZED COATED CONNECTION MATERIALS

        - As indicated on drawings.

        - Zinc-Coated Finish:  All items indicated for galvanizing, apply zinc coating by hot-dip process according to ASTM A 123/A 123M.

          - For steel shapes, plates, and tubing to be galvanized, limit silicon content of steel to less than 0.03 percent or to between 0.15 and 0.25 percent or limit sum of silicon and 2.5 times phosphorous content to 0.09 percent.

          - Galvanizing Repair Paint:  High-zinc-dust-content paint with dry film containing not less than 94 percent zinc dust by weight, and complying with DOD-P-21035B or SSPC-Paint 20.

      - STAINLESS-STEEL CONNECTION MATERIALS

        - As indicated on drawings.

Delete this Article if not required.  Retain when resistance to staining merits extra cost in parking structures and other high-moisture or corrosive areas.

        - Stainless-Steel Plate:  ASTM A 666, Type 304, of grade suitable for application.

        - Stainless-Steel Bolts and Studs:  ASTM F 593, Alloy 304 or 316, hex-head bolts and studs; stainless-steel nuts; and flat, stainless-steel washers.

          - Lubricate threaded parts of stainless-steel bolts with an antiseize thread lubricant during assembly.

        - Stainless-Steel-Headed Studs:  ASTM A 276, with minimum mechanical properties of PCI MNL 117, Table 3.2.3.

      - BEARING PADS

Delete this Article if not applicable.  Choice of bearing pad can usually be left to fabricator; coordinate selection with structural engineer if required.

        - Provide one of the following bearing pads for architectural precast concrete units[ as recommended by precast fabricator for application:

          - Elastomeric Pads:  AASHTO M 251, plain, vulcanized, 100 percent polychloroprene (neoprene) elastomer, molded to size or cut from a molded sheet, Type A durometer hardness of 50 to 70, ASTM D 2240, minimum tensile strength 2250 psi, ASTM D 412.

          - Random-Oriented, Fiber-Reinforced Elastomeric Pads:  Preformed, randomly oriented synthetic fibers set in elastomer.  Type A durometer hardness of 70 to 90, ASTM D 2240; capable of supporting a compressive stress of 3000 psi with no cracking, splitting, or delaminating in the internal portions of pad.  Test one specimen for every 200 pads used in Project.

          - Cotton-Duck-Fabric-Reinforced Elastomeric Pads:  Preformed, horizontally layered cotton-duck fabric bonded to an elastomer; Type A durometer hardness of 80 to 100, ASTM D 2240; complying with AASHTO's "AASHTO Load and Resistance Factor Design (LRFD) Bridge Design Specifications, Division II, Section 18.10.2, or with MIL-C-882E.

          - Frictionless Pads:  Tetrafluoroethylene (Teflon), glass-fiber reinforced, bonded to stainless or mild-steel plate, of type required for in-service stress.

          - High-Density Plastic:  Multimonomer, nonleaching, plastic strip.

      - ACCESSORIES

        - Reglets:  Specified in Division 07 Section "Sheet Metal Flashing And Trim."

Select paragraph above or first paragraph below if applicable.  Coordinate reglet material with counterflashing materials and details.

        - Precast Accessories:  Provide clips, hangers, plastic or steel shims, and other accessories required to install architectural precast concrete units.

        - Stair Nosings:  Consisting of an abrasive filler bonded and locked into channels in an extruded aluminum base, alloy 6063-T6.  Coefficient of friction 1.02 dry and .098 wet per ASTM standard F-609 Provide the following:

          - Basis of design:

            - Balco Inc.

          - Alternate acceptable Manufacturers:

            - American Safety Inc.

            - Wooster Products Inc.

      - GROUT MATERIALS

Add other proprietary grout systems to suit Project.  Show locations of each grout here or on Drawings if retaining more than one type.

        - Sand-Cement Grout:  Portland cement, ASTM C 150, Type I, and clean, natural sand, ASTM C 144 or ASTM C 404.  Mix at ratio of 1 part cement to 2-1/2 parts sand, by volume, with minimum water required for placement and hydration.

Retain first paragraph below if nonshrink grout is required or if cement-grout shrinkage could cause structural deficiency.  For critical installations, require manufacturer to provide field supervision.

        - Nonmetallic, Nonshrink Grout:  Premixed, nonmetallic, noncorrosive, nonstaining grout containing selected silica sands, portland cement, shrinkage-compensating agents, plasticizing and water-reducing agents, complying with ASTM C 1107, Grade A for drypack and Grades B and C for flowable grout and of consistency suitable for application within a 30-minute working time.

        - Epoxy-Resin Grout:  Two-component, mineral-filled epoxy resin; ASTM C 881/C 881M, of type, grade, and class to suit requirements.

        - Bond Breaker:  [Preformed, compressible, resilient, nonstaining, nonwaxing, closed-cell polyethylene foam pad, nonabsorbent to liquid and gas, 1/8 inch thick Polyethylene sheet, ASTM D 4397, 6 to 10 mils thick.

      - CONCRETE MIXTURES

        - Prepare design mixtures for each type of precast concrete required.

Revise subparagraph below if fly ash, silica fume, or metakaolin and silica fume are permitted.  Revise percentages to suit Project.

          - Limit use of fly ash and silica fume to 20 percent of portland cement by weight; limit metakaolin and silica fume to 10 percent of portland cement by weight.

        - Design mixtures may be prepared by a qualified independent testing agency or by qualified precast plant personnel at architectural precast concrete fabricator's option.

        - Limit water-soluble chloride ions to maximum percentage by weight of cement permitted by ACI 318 or PCI MNL 117 when tested according to ASTM C 1218/C 1218M.

Architectural precast concrete units may be manufactured with a separate architectural face mixture and a structural backup mixture.  Face and backup mixtures should have similar shrinkage and expansion coefficients.  Similar water-cementitious materials ratios and cement-aggregate ratios are recommended by PCI to limit bowing or warping.  Retain first option in paragraph below if lightweight backup concrete mix is required; second option if normal-weight face and backup mixtures are required; third option if full-depth, normal-weight mixture is required; or fourth option if choice of normal-weight face and backup mixtures or full-depth mixtures is fabricator's option.

        - Normal-Weight Concrete Mixtures:  Proportion full-depth mixtures, at fabricator's option by either laboratory trial batch or field test data methods according to ACI 211.1, with materials to be used on Project, to provide normal-weight concrete with the following properties:

Retain subparagraph below or revise to suit Project.  Higher-strength mixtures may be available; verify availability with fabricators.

          - Compressive Strength (28 Days):  5000 psi minimum.

Water-cementitious materials ratio of 0.40 to 0.45 is usual for architectural precast concrete.  Lower ratios may be possible with use of high-range water reducers.  Revise ratio in subparagraph below to suit Project.

          - Maximum Water-Cementitious Materials Ratio:  0.45.

Water absorption indicates susceptibility to weather staining.  PCI states that limits in paragraph below are suitable for average exposures.  Different parts of a single panel cannot be produced with different absorptions.  Verify that fabricators can produce units with lower water absorption because special consolidation techniques to increase concrete density are required.

        - Water Absorption:  6 percent by weight or 14 percent by volume, tested according to PCI MNL 117.

Retain subparagraph below or revise to suit Project.  Higher-strength mixtures may be available; verify availability with fabricators.

          - Compressive Strength (28 Days):  5000 psi.

Increase or decrease unit weight in subparagraph below to suit Project.  Coordinate with lightweight-aggregate supplier and architectural precast concrete fabricator.  Lightweight concretes with lightweight and normal-weight aggregate in mixture will usually be heavier than unit weight below.

          - Unit Weight:  Calculated equilibrium unit weight of 115 lb/cu. ft., plus or minus 3 lb/cu. ft., according to ASTM C 567.

        - Add air-entraining admixture at manufacturer's prescribed rate to result in concrete at point of placement having an air content complying with PCI MNL 117.

        - When included in design mixtures, add other admixtures to concrete mixtures according to manufacturer's written instructions.

      - MOLD FABRICATION

        - Molds:  Accurately construct molds, mortar tight, of sufficient strength to withstand pressures due to concrete-placement operations and temperature changes.  Coat contact surfaces of molds with release agent before reinforcement is placed.  Avoid contamination of reinforcement s by release agent.

Delete form liners in subparagraph below unless needed to produce exposed surface finish.

          - Place form liners accurately to provide finished surface texture indicated.  Provide solid backing and supports to maintain stability of liners during concrete placement.  Coat form liner with form-release agent.

        - Maintain molds to provide completed architectural precast concrete units of shapes, lines, and dimensions indicated, within fabrication tolerances specified.

          - Form joints are not permitted on faces exposed to view in the finished work.

Select one option from subparagraph below; show details on Drawings or revise description to add dimensions.  Sharp edges or corners of precast concrete units are vulnerable to chipping.

          - Edge and Corner Treatment:  Uniformly chamfered and/or radiused.

      - FABRICATION

        - Cast-in Anchors, Inserts, Plates, Angles, and Other Anchorage Hardware:  Fabricate anchorage hardware with sufficient anchorage and embedment to comply with design requirements.  Locate anchorage hardware where it does not affect position of main reinforcement or concrete placement.

          - Weld-headed studs and deformed bar anchors used for anchorage according to AWS D1.1/D1.1M and AWS C5.4, "Recommended Practices for Stud Welding."

Coordinate first paragraph below with Division 05 Section "Metal Fabrications" for furnishing and installing loose hardware items.

        - Furnish loose hardware items including steel plates, clip angles, seat angles, anchors, dowels, cramps, hangers, and other hardware shapes for securing architectural precast concrete units to supporting and adjacent construction.

        - Cast-in reglets, slots, holes, and other accessories in architectural precast concrete units as indicated on the Contract Drawings.

Delete first paragraph below if not applicable.

        - Cast-in openings in any dimension.  Do not drill or cut openings without Architect's approval.

        - Reinforcement:  Comply with recommendations in PCI MNL 117 for fabricating, placing, and supporting reinforcement.

          - Clean reinforcement of loose rust and mill scale, earth, and other materials that reduce or destroy the bond with concrete.  When damage to epoxy-coated reinforcing exceeds limits specified in ASTM A 775/A 775M, repair with patching material compatible with coating material and epoxy coat bar ends after cutting.

          - Accurately position, support, and secure reinforcement against displacement during concrete-placement and consolidation operations.  Completely conceal support devices to prevent exposure on finished surfaces.

          - Place reinforcement to maintain at least 3/4-inch -minimum coverage.  Arrange, space, and securely tie bars and bar supports to hold reinforcement in position while placing concrete.  Direct wire tie ends away from finished, exposed concrete surfaces.

          - Place reinforcing steel to maintain at least 3/4-inch -minimum concrete cover.  Increase cover requirements for reinforcing steel to 1-1/2-inches when units are exposed to corrosive environment or severe exposure conditions.  Arrange, space, and securely tie bars and bar supports to hold reinforcement in position while placing concrete.  Direct wire tie ends away from finished, exposed concrete surfaces.

          - Install welded wire fabric in lengths as long as practicable.  Lap adjoining pieces at least one full mesh spacing and wire tie laps, where required by design.  Offset laps of adjoining widths to prevent continuous laps in either direction.

        - Reinforce architectural precast concrete units to resist handling, transportation, and erection stresses.

Delete first paragraph and subparagraphs below if no precast, prestressed architectural concrete units are required.  Option to prestress may be left to fabricator if objective is to aid handling and to control cracking of units during installation.

        - Comply with requirements in PCI MNL 117 and requirements in this Section for measuring, mixing, transporting, and placing concrete.  After concrete batching, no additional water may be added.

Retain first paragraph below if a separate face mixture is required or is Contractor's option.

        - Place face mixture to a minimum thickness after consolidation of the greater of 1 inch or 1.5 times the maximum aggregate size, but not less than the minimum reinforcing cover specified.

        - Place concrete in a continuous operation to prevent seams or planes of weakness from forming in precast concrete units.

          - Place backup concrete mixture to ensure bond with face-mixture concrete.

        - Thoroughly consolidate placed concrete by internal and external vibration without dislocating or damaging reinforcement and built-in items, and minimize pour lines, honeycombing, or entrapped air on surfaces.  Use equipment and procedures complying with PCI MNL 117.

          - Place self-consolidating concrete without vibration according to PCI TR-6, "Interim Guidelines for the Use of Self-Consolidating Concrete in Precast/Prestressed Concrete Institute Member Plants."

        - Comply with PCI MNL 117 for hot- and cold-weather concrete placement.

        - Identify pickup points of architectural precast concrete units and orientation in structure with permanent markings, complying with markings indicated on Shop Drawings.  Imprint or permanently mark casting date on each architectural precast concrete unit on a surface that will not show in finished structure.

        - Cure concrete, according to requirements in PCI MNL 117, by moisture retention without heat or by accelerated heat curing using low-pressure live steam or radiant heat and moisture.  Cure units until compressive strength is high enough to ensure that stripping does not have an effect on performance or appearance of final product.

        - Discard and replace architectural precast concrete units that do not comply with requirements, including structural, manufacturing tolerance, and appearance, unless repairs meet requirements in PCI MNL 117 and Architect's approval.

      - FABRICATION TOLERANCES

        - Fabricate architectural precast concrete units straight and true to size and shape with exposed edges and corners precise and true so each finished panel complies with PCI MNL 117 product tolerances as well as position tolerances for cast-in items.

Select paragraph above or first paragraph and subparagraphs below.  PCI MNL 117 product tolerances, referenced above and listed below, are standardized throughout the industry.

        - Fabricate architectural precast concrete units straight and true to size and shape with exposed edges and corners precise and true so each finished panel complies with the following product tolerances:

          - Overall Height and Width of Units, Measured at the Face Exposed to View:  As follows:

            - 10-feet or under, plus or minus 1/8-inch.

            - 10 to 20-feet, plus 1/8-inch (3mm), minus 3/16-inch.

            - 20 to 40-feet  plus or minus 1/4-inch

            - Each additional 10-feet, plus or minus 1/16-inch.

          - Overall Height and Width of Units, Measured at the Face Not Exposed to View:  As follows:

            - 10-feet or under, plus or minus 1/4-inch.

            - 10 to 20-feet, plus 1/4-inch, minus 3/8-inch.

            - 20 to 40-feet, plus or minus 3/8-inch.

            - Each additional 10-feet, plus or minus 1/8-inch.

          - Total Thickness or Flange Thickness:  Plus 1/4-inch, minus 1/8-inch.

          - Rib Thickness:  Plus or minus 1/8-inch.

          - Rib to Edge of Flange:  Plus or minus 1/8-inch.

          - Distance between Ribs:  Plus or minus 1/8-inch.

          - Variation from Square or Designated Skew (Difference in Length of the Two Diagonal Measurements):  Plus or minus 1/8-inch per 72-inches or 1/2-inch total, whichever is greater.

          - Length and Width of Block-outs and Openings within One Unit:  Plus or minus 1/4-inch.

          - Location and Dimension of Block-outs Hidden from View and Used for HVAC and Utility Penetrations:  Plus or minus 3/4-inch.

          - Dimensions of Haunches:  Plus or minus 1/4-inch.

          - Haunch Bearing Surface Deviation from Specified Plane:  Plus or minus 1/8-inch.

          - Difference in Relative Position of Adjacent Haunch Bearing Surfaces from Specified Relative Position:  Plus or minus 1/4 inch.

          - Bowing:  Plus or minus L/360, maximum 1-inch.

          - Local Smoothness:  1/4-inch per 10-feet.

          - Warping:  1/16-inch per 12-inches of distance from nearest adjacent corner.

          - Tipping and Flushness of Plates:  Plus or minus 1/4-inch.

          - Dimensions of Architectural Features and Rustications:  Plus or minus 1/8-inch.

        - Position Tolerances:  For cast-in items measured from datum line location, as indicated on Shop Drawings.

          - Weld Plates:  Plus or minus 1-inch.

          - Inserts:  Plus or minus 1/2-inch.

          - Handling Devices:  Plus or minus 3-inches.

          - Reinforcing Steel and Welded Wire Fabric:  Plus or minus 1/4-inch where position has structural implications or affects concrete cover; otherwise, plus or minus 1/2-inch.

          - Reinforcing Steel Extending out of Member:  Plus or minus 1/2-inch of plan dimensions.

          - Tendons:  Plus or minus 1/4-inch, vertical; plus or minus 1-inch, horizontal.

          - Location of Rustication Joints:  Plus or minus 1/8-inch.

          - Location of Opening within Panel:  Plus or minus 1/4-inch.

          - Location of Flashing Reglets:  Plus or minus 1/4-inch.

          - Location of Flashing Reglets at Edge of Panel:  Plus or minus 1/8-inch.

          - Reglets for Glazing Gaskets:  Plus or minus 1/8-inch.

          - Electrical Outlets, Hose Bibs:  Plus or minus 1/2-inch.

          - Location of Bearing Surface from End of Member:  Plus or minus 1/4-inch.

          - Allowable Rotation of Plate, Channel Inserts, and Electrical Boxes:  2-degree rotation or 1/4-inch (6mm) maximum over the full dimension of unit.

          - Position of Sleeve:  Plus or minus 1/2-inch.

          - Location of Window Washer Track or Buttons:  Plus or minus 1/8-inch.

Delete paragraph and subparagraphs below if stone veneer-faced architectural precast units are not used.

      - FINISHES

        - Panel faces shall be free of joint marks, grain, and other obvious defects.  Corners, including false joints shall be uniform, straight, and sharp.  Finish exposed-face surfaces of architectural precast concrete units to match approved design reference sample and as follows:

This Article presumes Architect has preapproved one or more design reference samples.  Include complete description of design reference sample here.  If preapproving fabricators, coordinate with "Manufacturers" Article.  Revise if multiple samples are approved.

          - Design Reference Sample provided by Northwest Precast approved by architect

Delete subparagraph below if not required.  If retaining, revise and add reference number; PCI publishes numbered, color photographs of 428 precast concrete finishes; see PCI's Web site, www.pci.org.  Add reference number combinations if more than one finish is required.

Select type of finish from subparagraphs below if needed.  If more than one finish is required, add locations to finish descriptions or indicate on Drawings.  Add more-detailed descriptions of finishes outlined below if greater definition, such as light, medium, or deep, is required,.  See PCI MNL 117 for more information on finishes.  An as-cast finish generally results in a mottled surface or non-uniform finish.

          - As-Cast Surface Finish:  Provide surfaces free of pockets, sand streaks, and honeycombs.

          - Textured-Surface Finish:  Impart by form liners or inserts to provide surfaces free of pockets, streaks, and honeycombs, with uniform color and texture.

          - Bushhammer Finish:  Use power or hand tools to remove matrix and fracture coarse aggregates.

          - Exposed-Aggregate Finish:  Use chemical retarding agents applied to concrete forms and washing and brushing procedures to expose aggregate and surrounding matrix surfaces after form removal.

          - Abrasive-Blast Finish:  Use abrasive grit, equipment, application techniques, and cleaning procedures to expose aggregate and surrounding matrix surfaces.

          - Acid-Etched Finish:  Use acid and hot-water solution, equipment, application techniques, and cleaning procedures to expose aggregate and surrounding matrix surfaces.  Protect hardware, connections, and insulation from acid attach.

          - Honed Finish:  Use continuous mechanical abrasion with fine grit, followed by filling and rubbing procedures.

          - Polished Finish:  Use continuous mechanical abrasion with fine grit, followed by filling and rubbing procedures.

          - Sand-Embedment Finish:  Use selected stones placed in a sand bed in bottom of mold, with sand removed after curing.

        - Finish exposed as indicated on drawings surfaces of architectural precast concrete units to match face-surface finish.

Retain paragraph above or below if applicable.  Revise below to float finish or light-broom finish if smooth, steel-trowel finish is unnecessary.

        - Finish exposed indicated on drawings surfaces of architectural precast concrete units by smooth, steel-trowel finish.

Revise finish in paragraph below to light-broom, stippled, or as-cast finish if float finish is unnecessary, or upgrade to smooth, steel-trowel finish.

        - Finish unexposed surfaces of architectural precast concrete units by float finish.

      - FACTORY APPLIED SEALERS AND COATINGS

Retain paragraph below if establishing a minimum standard of plant testing and inspecting.  PCI MNL 117 mandates source testing requirements and a plant "Quality Systems Manual."  PCI certification also ensures periodic auditing of plants for compliance with requirements in PCI MNL 117.

        - Concrete Coatings, water repellants.  High performance factory applied coatings as follows:

        - 1.  Low VOC type; colorless, pure silane water repellant penetrating sealers.

            - Hydrozo 100 High performance sealer

        - 3. Sealer to maintain natural look of concrete surface with no glaze or gloss, darkening of color change.

        - E.	Graffiti control:  if indicated by drawings.

      - SOURCE QUALITY CONTROL

Retain paragraph below if establishing a minimum standard of plant testing and inspecting.  PCI MNL 117 mandates source testing requirements and a plant "Quality Systems Manual."  PCI certification also ensures periodic auditing of plants for compliance with requirements in PCI MNL 117.

        - Quality-Control Testing:  Test and inspect precast concrete according to PCI MNL 117 requirements.  If using self-consolidating concrete, also test and inspect according to PCI TR-6, "Interim Guidelines for the Use of Self-Consolidating Concrete in Precast/Prestressed Concrete Institute Member Plants."

Delete first paragraph and subparagraph below if not required.  PCI certification may be acceptable to authorities having jurisdiction without further monitoring of plant quality-control and testing program by Owner.

        - Owner will employ an independent testing agency to evaluate architectural precast concrete fabricator's quality-control and testing methods.

          - Allow Owner's testing agency access to material storage areas, concrete production equipment, concrete placement, and curing facilities.  Cooperate with Owner's testing agency and provide samples of materials and concrete mixtures as may be requested for additional testing and evaluation.

        - Strength of precast concrete units will be considered deficient if units fail to comply with ACI 318 requirements for concrete strength.

Review testing and acceptance criteria with structural engineer.  In first paragraph and subparagraphs below, add criteria for load tests if required.

        - Testing:  If there is evidence that strength of precast concrete units may be deficient or may not comply with ACI 318 requirements, precaster will employ an independent testing agency to obtain, prepare, and test cores drilled from hardened concrete to determine compressive strength according to ASTM C 42/C 42M.

          - A minimum of three representative cores will be taken from units of suspect strength, from locations directed by Architect.

          - Cores will be tested in an air-dry condition.

PCI's recommendations in first subparagraph below are more stringent than ACI's.

          - Strength of concrete for each series of 3 cores will be considered satisfactory if average compressive strength is equal to at least 85 percent of 28-day design compressive strength and no single core is less than 75 percent of 28-day design compressive strength.

          - Test results will be made in writing on same day that tests are performed, with copies to Architect, Contractor, and precast concrete fabricator.  Test reports will include the following:

            - Project identification name and number.

            - Date when tests were performed.

            - Name of precast concrete fabricator.

            - Name of concrete testing agency.

            - Identification letter, name, and type of precast concrete unit(s) represented by core tests; design compressive strength; type of break; compressive strength at breaks, corrected for length-diameter ratio; and direction of applied load to core in relation to horizontal plane of concrete as placed.

        - Patching:  If core test results are satisfactory and precast concrete units comply with requirements, clean and dampen core holes and solidly fill with precast concrete mixture that has no coarse aggregate, and finish to match adjacent precast concrete surfaces.

- EXECUTION

      - EXAMINATION

        - Examine supporting structural frame or foundation and conditions for compliance with requirements for installation tolerances, true and level bearing surfaces, and other conditions affecting performance.

        - Proceed with installation only after unsatisfactory conditions have been corrected.

        - Do not install precast concrete units until supporting cast-in-place building structural framing has attained minimum allowable design compressive strength or supporting steel or other structure is complete.

      - INSTALLATION

        - Install clips, hangers, bearing pads, and other accessories required for connecting architectural precast concrete units to supporting members and backup materials.

        - Erect architectural precast concrete level, plumb, and square within specified allowable tolerances.  Provide temporary supports and bracing as required to maintain position, stability, and alignment as units are being permanently connected.

          - Install temporary steel or plastic spacing shims or bearing pads as precast concrete units are being erected.  Tack weld steel shims to each other to prevent shims from separating.

          - Maintain horizontal and vertical joint alignment and uniform joint width as erection progresses.

          - Remove projecting lifting devices and grout fill voids within recessed lifting devices flush with surface of adjacent precast surfaces when recess is exposed.

          - Unless otherwise indicated, maintain uniform joint widths of 3/4-inch.

        - Connect architectural precast concrete units in position by bolting, welding, grouting, or as otherwise indicated on Shop Drawings.  Remove temporary shims, wedges, and spacers as soon as practical after connecting and grouting are completed.

          - Do not permit connections to disrupt continuity of roof flashing.

        - Welding:  Comply with applicable AWS D1.1/D1.1M and AWS D1.4 for welding, welding electrodes, appearance, quality of welds, and methods used in correcting welding work.

          - Protect architectural precast concrete units and bearing pads from damage by field welding or cutting operations, and provide noncombustible shields as required.

          - Welds not specified shall be continuous fillet welds, using no less than the minimum fillet as specified by AWS.

          - Clean weld-affected metal surfaces with chipping hammer followed by brushing, and apply a minimum 4.0-mil -thick coat of galvanized repair paint to galvanized surfaces according to ASTM A 780.

Retain last subparagraph above or first subparagraph below.

          - Clean weld-affected metal surfaces with chipping hammer followed by brushing, and reprime damaged painted surfaces.

          - Remove, reweld, or repair incomplete and defective welds.

        - At bolted connections, use lock washers, tack welding, or other approved means to prevent loosening of nuts after final adjustment.

          - Where slotted connections are used, verify bolt position and tightness.  For sliding connections, properly secure bolt but allow bolt to move within connection slot.  For friction connections, apply specified bolt torque and check 25 percent of bolts at random by calibrated torque wrench.

In paragraph below, revise locations and extent of grouting if required.

        - Grouting Connections:  Grout connections where required or indicated.  Retain grout in place until hard enough to support itself.  Pack spaces with stiff grout material, tamping until voids are completely filled.  Place grout to finish smooth, level, and plumb with adjacent concrete surfaces.  Keep grouted joints damp for not less than 24 hours after initial set.  Promptly remove grout material from exposed surfaces before it affects finishes or hardens.

      - ERECTION TOLERANCES

        - Erect architectural precast concrete units level, plumb, square, true, and in alignment without exceeding the noncumulative erection tolerances of PCI MNL 117, Appendix I.

Select paragraph above or paragraph and subparagraphs below.  Usually retain above unless tolerances for Project deviate from PCI recommendations.  PCI MNL 117 erection tolerances are referenced above and listed below.

        - Erect architectural precast concrete units level, plumb, square, and true, without exceeding the following noncumulative erection tolerances:

          - Plan Location from Building Grid Datum:  Plus or minus 1/2-inch.

          - Plan Location from Centerline of Steel:  Plus or minus 1/2-inch.

          - Top Elevation from Nominal Top Elevation:  As follows:

            - Exposed Individual Panel:  Plus or minus 1/4-inch.

            - Non-Exposed Individual Panel:  Plus or minus 1/2-inch.

            - Exposed Panel Relative to Adjacent Panel:  1/4-inch.

            - Non-Exposed Panel Relative to Adjacent Panel:  1/2-inch.

          - Support Elevation from Nominal Support Elevation:  As follows:

            - Maximum Low:  1/2-inch.

            - Maximum High:  1/4-inch.

          - Maximum Plumb Variation over the Lesser of Height of Structure or 100-Feet:  1-inch.

          - Plumb in Any 10 Feet of Element Height:  1/4-inch.

          - Maximum Jog in Alignment of Matching Edges:  1/4-inch.

          - Joint Width (Governs over Joint Taper):  Plus or minus 1/4-inch.

          - Maximum Joint Taper:  3/8-inch.

          - Joint Taper in 10-Feet:  1/4-inch.

          - Maximum Jog in Alignment of Matching Faces:  1/4-inch.

          - Differential Bowing or Camber, as Erected, between Adjacent Members of Same Design:  1/4-nch.

          - Opening Height between Spandrels:  Plus or minus 1/4-nch.

      - FIELD QUALITY CONTROL

Retain first option in paragraph below if Owner engages a special inspector.  If authorities having jurisdiction permit Contractor to engage a special inspector, retain second option and retain option for submitting special inspection reports in Part 1 "Informational Submittals" Article.

        - Special Inspections:  Owner will engage a qualified special inspector to perform the following special inspections and prepare reports:

          - Erection of precast concrete members.

Retain first paragraph below, with or without paragraph above, to identify who shall perform tests and inspections.  If retaining second option, retain requirement for field quality-control test reports in Part 1 "Informational Submittals" Article.

        - Testing Agency:  Owner will engage a qualified testing agency to perform tests and inspections and prepare test reports.

        - Field welds will be subject to visual inspections and nondestructive testing according to ASTM E 165 or ASTM E 709.  High-strength bolted connections will be subject to inspections.

        - Testing agency will report test results promptly and in writing to Contractor and Architect.

        - Repair or remove and replace work where tests and inspections indicate that it does not comply with specified requirements.

        - Additional testing and inspecting, at Contractor's expense, will be performed to determine compliance of replaced or additional work with specified requirements.

      - REPAIRS

Blemishes occurring after delivery are normally repaired before final joint sealing and cleaning as weather permits.

        - Repair architectural precast concrete units if permitted by Architect.  The Architect reserves the right to reject repaired units that do not comply with requirements.

Precast concrete manufacturer should develop appropriate repair mixtures and techniques during production sample approval process.

        - Mix patching materials and repair units so cured patches blend with color, texture, and uniformity of adjacent exposed surfaces and show no apparent line of demarcation between original and repaired work, when viewed in typical daylight illumination from a distance of 20 feet .

Retain paragraph above if using galvanized anchors, connections, and other items; retain first paragraph below if items are prime painted.

        - Wire brush, clean, and paint damaged prime-painted components with same type of shop primer.

        - Remove and replace damaged architectural precast concrete units when repairs do not comply with requirements.

      - CLEANING

        - Clean surfaces of precast concrete units exposed to view.

        - Clean mortar, plaster, fireproofing, weld slag, and other deleterious material from concrete surfaces and adjacent materials immediately.

        - Clean exposed surfaces of precast concrete units after erection and completion of joint treatment to remove weld marks, other markings, dirt, and stains.

          - Perform cleaning procedures, if necessary, according to precast concrete fabricator's recommendations.  Clean soiled precast concrete surfaces with detergent and water, using stiff fiber brushes and sponges, and rinse with clean water.  Protect other work from staining or damage due to cleaning operations.

          - Do not use cleaning materials or processes that could change the appearance of exposed concrete finishes or damage adjacent materials.

- END OF SECTION 034500